## Slide 1
Trenchless Stormwater Culvert Rehabilitation
Jaco Griessel

## Slide 2: CIPP Rehabilitation
Over View

## Slide 7
CIPP Liner Materials – Resin
Note: HDPE PE 100 has a flexural modulus of 1,000 MPa and PVC has a flexural modulus 3,500-4,500 Mpa.

## Slide 8
CIPP liner materials – comparison for DN1200 Culvert
NCI DN1200 Culvert Design Calculations |  |  | 
Design category | Standard Felt CIPP | Composite Reinforced Felt CIPP | Fibreglass (UV)
Flexural Modulus | 2,200 MPa | 27,400 MPa | 13,600 MPa
Flexural Strength | 37.5 MPa | 113.5 MPa | 200 MPa
Wall Thickness | 35.5mm | 23.8mm | 16.5mm
Resin Quantities | 24,400kg | 16,600kg | 11,800kg
Net Weight | 29,600kg | 21,200kg | 15,500kg
Material Cost | $ | $$ | $$$
Installation Cost | $$ | $$ | $
 | MATERIAL COST = LOW INSTALLATION COST = HIGH EXTRA WORKERS ON SITE |  | MATERIAL COST = HIGH INSTALLATION COST = LOW FASTER TO INSTALL WITH LESS WORKERS

## Slide 10
Water Cured CIPP – Waiawaka Culvert

## Slide 11
Water Cured CIPP – Waiawaka Culvert
Liner Selection:
Shape of existing culvert 734mm x 1258mm
Thickness needed for structural design 45mm
UV light spacing would not have been able to be centralised in this instance

## Slide 12
Water Cured CIPP – Waiawaka Culvert

## Slide 13
Water Cured CIPP – Waiawaka Culvert
Final Design 46mm Wall Thickness

## Slide 14
Water Cured CIPP – Waiawaka Culvert

## Slide 15
Water Cured CIPP – Waiawaka Culvert

## Slide 16
UV Cured – NCI
1200mm dia UV Cured
160m long
2 day installation

## Slide 17
UV Cured – NCI
SITE CONSTRAINTS
Multi contractor shared site
with concurrent works
Reduced construction space
Site well suited to minimal
establishment, reduced
onsite plant and materials
  UV

## Slide 18
UV Cured – NCI
DESIGN CONSIDERATIONS
Maximise flow capacity by utilising the thinnest applicable liner
Six month shelf life of material allowing versatility in installation timing
Lighter weight of materials/ less manual handling
Less onsite staff
Small site footprint

## Slide 19
UV Cured – NCI

## Slide 20
UV Cured – NCI

## Slide 21
UV Cured – NCI

## Slide 22
UV Cured – NCI

## Slide 23
UV Cured – NCI