## Slide 1: Nuflow Australasia
CIPP & SIPP pipe relining solutions

## Slide 2: Topics- Dr David Rogers Polymer Chemist
UV curing – epoxy and non-epoxy
Mechanical properties and future use of fibreglass
Chemistry differences
“dark cure”
similarities
ASTM F1216 minimum structural requirements
Relative flexural properties of neat resin; felt and fibreglass
Upcoming pressure and structural standards
Necessity for fibreglass and advanced fibre liners

## Slide 3: Free radical vs cationic cure
Free radical cure: light splits molecule to create radicals that begin cure
Cationic cure: light creates strong acid
that begins cure
Polyester / vinyl ester / acrylic resins
Epoxy resins

## Slide 4: UV epoxy
“Dark cure”
Cure can continue after light is removed
UV cure similarities: epoxy / non-epoxy
Nearly indefinite pot-life / working time
Very rapid cure

## Slide 5: UV cure
Nuflow USA – Australia synergy
Works with non-epoxy (395nm) and epoxy (365nm) resins
Capable of DN100 or DN150 liner cure within 10-15 minutes
UV epoxy 100% solids (no volatiles)
UV epoxy excellent adhesion to host pipe: necessary for some structural requirements

## Slide 6: Liner reinforcements
Subheading
- ASTM F1216, first published 1989
- Modest structural properties

## Slide 7: AWWA Structural Classification of Pressure Pipe Linings, 2019
Class I: non-structural (spray coat, resin/felt)
Class II: adhesion to host pipe (epoxy)
Class III: high ring stiffness to withstand vacuum / hydraulic pressure
Class IV: fully structural independent of host pipe

## Slide 8: Structural properties of liners
Neat resin; felt; fiberglass
Neat resin is stronger and stiffer than resin / felt
Fibreglass can massively increase strength / stiffness of resin
Greater stiffness of fibreglass / resin means thinner liners can be used
Thinner liners means much less resin needs to be used, lowering weight & cost

## Slide 9: Floreana Coman Reinforcements overview and Novelties for CIPP

## Slide 10: The Properties of Fibre Reinforced Plastics (FRP)/Composite Materials
Overall, the properties of a composites are determined by:
  - Properties of fibres
  - The ratio of fibre-to-resin in the composite ( Fibre Volume fraction Vf)
  - Type, Geometry and Orientation of the fibres in the composite
  - Properties of resins
  - Manufacturing method

## Slide 11: COMPARISON High Tech Fibres’ Strengths & Weaknesses
Property | Carbon | Aramid | Glass
Tensile Strength | 1 | 2 | 2
Tensile Modulus | 1 | 2 | 3
Compressive Strength | 1 | 3 | 2
Compressive Modulus | 1 | 2 | 3
Flexural Strength (see photo) | 2 | 1 | 3
Flexural Modulus | 1 | 3 | 2
Impact Strength | 3 | 1 | 2
Inter-laminar Shear Strength | 1 | 2 | 1
In-plane Shear Strength | 1 | 2 | 1
Density | 2 | 1 | 3
Fatigue Resistance | 1 | 2 | 3
Fire Resistance | 1 | 2 | 1
Thermal Expansion | 1 | 2 | 2
Thermal Insulation | 3 | 1 | 2
Electrical Insulation | 3 | 2 | 1

## Slide 12: FIBRE REINFORCEMENTS Format: 1.Continuous 2.Randomly dispersed (nonwoven, CSM) 3.Combination of 1 & 2 by stitching,

## Slide 13: Continuous REINFORCEMENTS
  2D Woven fabrics. Weave patterns describes the way warp and weft threads are interlaced with each other Warp and weft: The threads that run along the length of the fabric are called warp/ ends The threads that run from selvedge to selvedge are called weft/ picks
      - Plain
      -Twill
      - Satin
      - Combination

## Slide 14: Continuous REINFORCEMENTS
  Multiaxial uncrimped
      Unidirectional (0° )or ( 90°)
      Biaxial (0°, 90°)
      Triaxial (0°, ±45°) or (90°, ±45°)
      Double Bias (±45°)
      Quadriaxial (0°, ±45°,90°)

## Slide 15
Weft Filler Yarns
Layers 1 & 2
Warp Binder Yarns
Weft Weft Layers 1, 2 & 3
3D Fabrics (X Y Z)

## Slide 16: 3D weaving loom

## Slide 17: Nuflow 3 D weaving loom
The Manufacturing facility has now installed the Loom machine and will be commissioned within the next 3 months producing CIPP solutions.

## Slide 19: Novel 3D fabrics
3-D preforms style:
  “Non Crimp” multilayer
      up to 20 layers
      in a variety of architectures:
      orthogonal, interlayered, offset, etc.
      warp binding, weft binding

## Slide 20: Novel 3D Preforms
Profiled Fabrics T, I, C, U, Y ,L…

## Slide 21: THANK YOU
FOR MORE INFORMATION CONTACT
Jeff Hilditch National Business Development Manager Australasia
James Haua Technical Training & Development Australasia
solutions@nuflow.net
Nat